## Slide 1: Chemistry
Fifth Edition
Julia Burdge Lecture PowerPoints Chapter 24
Metallurgy and the Chemistry of Metals
Copyright © McGraw-Hill Education. All rights reserved. No reproduction or distribution without the prior written consent of McGraw-Hill Education.

## Slide 2: Metallurgy and the Chemistry of Metals
CHAPTER
24
24.1 Occurrence of Metals
24.2 Metallurgical Processes
24.3 Band Theory of Conductivity
24.4 Periodic Trends in Metallic Properties
24.5 The Alkali Metals
24.6 The Alkaline Earth Metals
24.7 Aluminum

## Slide 3: 24.1 Occurrence of Metals
Topics
Occurrence of Metals

## Slide 4: 24.1 Occurrence of Metals (1)
Occurrence of Metals

## Slide 5: 24.1 Occurrence of Metals (2)
Occurrence of Metals
Most metals come from minerals.
A mineral is a naturally occurring substance with a range of chemical composition.
A mineral deposit concentrated enough to allow economical recovery of a desired metal is known as ore.

## Slide 6: 24.2 Metallurgical Processes
Topics
Preparation of the Ore
Production of Metals
The Metallurgy of Iron
Steelmaking
Purification of Metals

## Slide 7: 24.2 Metallurgical Processes (1)
Preparation of the Ore
In the preliminary treatment of an ore, the desired mineral is separated from waste materials— usually clay and silicate minerals—which are collectively called the gangue.
One very useful method for carrying out such a separation is called flotation.
Another physical separation process makes use of the magnetic properties of certain minerals. Ferromagnetic metals are strongly attracted to magnets.

## Slide 8: 24.2 Metallurgical Processes (2)
Production of Metals
An ore may be roasted to drive off volatile impurities and at the same time to convert the carbonates and sulfides to the corresponding oxides :

## Slide 9: 24.2 Metallurgical Processes (3)
Production of Metals (in decreasing activity of metals)
TABLE 24.2 Reduction Processes for Some Common Metals
Metal | Reduction Process
Lithium, sodium, magnesium, calcium | Electrolytic reduction of the molten chloride
Aluminum | Electrolytic reduction of anhydrous oxide (in molten cryolite)
Chromium, manganese, titanium, vanadium, iron, zinc | Reduction of the metal oxide with a more electropositive metal, or reduction with coke and carbon monoxide
Mercury, silver, platinum, copper, gold | These metals occur in the free (uncombined) state, or they can be obtained by roasting their sulfides
Copyright © The McGraw-Hill Companies, Inc. Permission required for reproduction or display

## Slide 10: 24.2 Metallurgical Processes (4)
Production of Metals
Most major metallurgical processes now in use involve pyrometallurgy, procedures carried out at high temperatures.
The reduction in these procedures may be accomplished either chemically or electrolytically

## Slide 11: 24.2 Metallurgical Processes (5)
Production of Metals
Chemical Reduction

## Slide 12: 24.2 Metallurgical Processes (6)
Production of Metals
Electrolytic Reduction
Electrolytic reduction is suitable for very electropositive metals, such as sodium, magnesium, and aluminum.
The process is usually carried out on the anhydrous molten oxide or halide of the metal:

## Slide 13: 24.2 Metallurgical Processes (7)
The Metallurgy of Iron

## Slide 14: 24.2 Metallurgical Processes (8)
The Metallurgy of Iron
Iron extracted in this way contains many impurities and is called pig iron; it may contain up to 5 percent carbon and some silicon, phosphorus, manganese, and sulfur.

## Slide 15: 24.2 Metallurgical Processes (9)
Steelmaking
Whereas the production of iron is basically a reduction process (converting iron oxides to metallic iron), the conversion of iron to steel is essentially an oxidation process in which the unwanted impurities are removed from the iron by reaction with oxygen gas.

## Slide 16: 24.2 Metallurgical Processes (10)
Steelmaking

## Slide 17: 24.2 Metallurgical Processes (11)
Steelmaking
The type of flux chosen depends on the composition of the iron.
If the main impurities are silicon and phosphorus, a basic flux such as CaO is added to the iron:
If manganese is the main impurity, then an acidic flux such as SiO2 is needed to form the slag:

## Slide 18: 24.2 Metallurgical Processes (12)
Steelmaking
At high temperatures, iron and carbon in steel combine to form iron carbide (Fe3C), called cementite:
When steel containing cementite is cooled slowly, the preceding equilibrium shifts to the left and the carbon separates as small particles of graphite, which give the steel a grey color.

## Slide 19: 24.2 Metallurgical Processes (13)
Steelmaking
If the steel is cooled rapidly, equilibrium is not attained and the carbon remains largely in the form of cementite (Fe3C).
Steel containing cementite is light in color, and it is harder and more brittle than that containing graphite.

## Slide 20: 24.2 Metallurgical Processes (14)
Steelmaking
TABLE 24.3 Types of Steel - Composition (Percent by Mass)*
Type | C | MN | P | S | Si | Ni | Cr | Others | Users
Plain | 1.35 | 1.65 | 0.04 | 0.05 | 0.06 | ─ | ─ | Cu (0.2-0.6) | Sheet products, tools
High-strengh | 0.25 | 1.65 | 0.04 | 0.05 | 0.15 – 0.9 | 0.4 – 1.0 | 0.3 – 1.3 | Cu (0.01–0.08) | Construction, Steam turbines
Stainless | 0.03 – 1.2 | 1.0 – 10 | 0.04 – 0.06 | 0.03 | 1–3 | 1–22 | 4.0–27 | ─ | Kitchen utensils, Razor blades

## Slide 21: 24.2 Metallurgical Processes (15)
Purification of Metals
Distillation
Ni(CO)4(g)
Pure metallic nickel is recovered from Ni(CO)4 by heating the gas at 200°C:

## Slide 22: 24.2 Metallurgical Processes (16)
Purification of Metals
Electrolysis
Anode (oxidation):
Cathode (reduction):

## Slide 23: 24.2 Metallurgical Processes (17)
Purification of Metals
Zone Refining

## Slide 24: 24.3 Band Theory of Conductivity
Topics
Conductors
Semiconductors

## Slide 25: 24.3 Band Theory of Conductivity (1)
Conductors
The model we will use to study metallic bonding is band theory, so called because it states that delocalized electrons move freely through “bands” formed by overlapping molecular orbitals.
Conductors are capable of conducting an electric current.

## Slide 26: 24.3 Band Theory of Conductivity (2)
Conductors

## Slide 27: 24.3 Band Theory of Conductivity (3)
Semiconductors
Semiconductors are elements that normally are not conductors, but will conduct electricity at elevated temperatures or when combined with a small amount of certain other elements.
Insulators are ineffective conductors of electricity.

## Slide 28: 24.3 Band Theory of Conductivity (4)
Semiconductors

## Slide 29: 24.3 Band Theory of Conductivity (5)
Semiconductors
n-type semiconductor p-type semiconductor

## Slide 30: 24.4 Periodic Trends in Metallic Properties
Topics
Periodic Trends in Metallic Properties

## Slide 31: 24.4 Periodic Trends in Metallic Properties (1)
Periodic Trends in Metallic Properties
Main Group and Group 2B Metals

## Slide 32: 24.4 Periodic Trends in Metallic Properties (2)
Periodic Trends in Metallic Properties
Metals are lustrous in appearance, solid at room temperature (with the exception of mercury), good conductors of heat and electricity, malleable (can be hammered flat), and ductile (can be drawn into wires).
The electronegativity of elements increases from left to right across a period and from bottom to top in a group.
The metallic character of metals increases in just the opposite directions—that is, from right to left across a period and from top to bottom in a group.

## Slide 33: 24.4 Periodic Trends in Metallic Properties (3)
Periodic Trends in Metallic Properties
Because metals generally have low electronegativities, they tend to form cations and almost always have positive oxidation numbers in their compounds.
However, beryllium and magnesium in Group 2A and the metals in Group 3A and beyond also form covalent compounds.

## Slide 34: 24.5 The Alkali Metals
Topics
The Alkali Metals

## Slide 35: 24.5 The Alkali Metals (1)
The Alkali Metals
Table 24.4 Properties of Alkali Metals
 | Li | Na | K | Rb | Cs
Valence electron configuration | 2s1 | 3s1 | 4s1 | 5s1 | 6s1
Density (g/cm3) | 0.534 | 0.97 | 0.86 | 1.53 | 1.87
Melting point () | 179 | 97.6 | 63 | 39 | 28
Boiling point () | 1317 | 892 | 770 | 688 | 678
Atomic radius (pm) | 155 | 190 | 235 | 248 | 267
Ionic radius (pm)* | 60 | 95 | 133 | 148 | 169
Ionization energy (kJ/mol) | 520 | 496 | 419 | 403 | 375
Electronegativity | 1.0 | 0.9 | 0.8 | 0.8 | 0.7
Standard reduction potential (V)† | — 3.05 | — 2.71 | — 2.93 | — 2.93 | — 2.92
 | Li | Na | K | Rb | Cs
Valence electron configuration | 2s1 | 3s1 | 4s1 | 5s1 | 6s1
Density (g/cm3) | 0.534 | 0.97 | 0.86 | 1.53 | 1.87
 | 179 | 97.6 | 63 | 39 | 28
 | 1317 | 892 | 770 | 688 | 678
Atomic radius (pm) | 155 | 190 | 235 | 248 | 267
Ionic radius (pm)* | 60 | 95 | 133 | 148 | 169
Ionization energy (kJ/mol) | 520 | 496 | 419 | 403 | 375
Electronegativity | 1.0 | 0.9 | 0.8 | 0.8 | 0.7
Standard reduction potential (V)† | — 3.05 | — 2.71 | — 2.93 | — 2.93 | — 2.92

## Slide 36: 24.5 The Alkali Metals (2)
The Alkali Metals
Sodium Carbonate (Soda Ash)
Via Solvay Process:
From Trona:

## Slide 37: 24.5 The Alkali Metals (3)
The Alkali Metals
Potassium Nitrate (saltpeter) :
Gunpowder consists of potassium nitrate, wood charcoal, and sulfur in the approximate proportions of 6:1:1 by mass.

## Slide 38: 24.6 The Alkaline Earth Metals
Topics
Magnesium
Calcium

## Slide 39: 24.6 The Alkaline Earth Metals (1)
Table 24.5 Properties of Alkaline Earth Metals
 | Be | Mg | Ca | Sr | Ba
Valence electron configuration | 2s2 | 3s2 | 4s2 | 5s2 | 6s2
Density (g/cm3) | 1.86 | 1.74 | 1.55 | 2.6 | 3.5
Melting poing () | 1280 | 650 | 838 | 770 | 714
Boiling point () | 2770 | 1107 | 1484 | 1380 | 1640
Atomic radius (pm) | 112 | 160 | 197 | 215 | 222
Lonic radius (pm)* | 31 | 651 | 99 | 113 | 135
First ionization energy (kJ/mol) | 899 | 738 | 590 | 548 | 502
Second ionization energy (kJ/mol) | 1757 | 1450 | 1145 | 1058 | 958
Electronegativity | 1.5 | 1.2 | 1.0 | 1.0 | 0.9
Standard reduction potential (V)† | ─ 1.85 | ─ 2.37 | ─ 2.87 | ─ 2.89 | ─ 2.90
 | Be | Mg | Ca | Sr | Ba
Valence electron configuration | 2s2 | 3s2 | 4s2 | 5s2 | 6s2
Density (g/cm3) | 1.86 | 1.74 | 1.55 | 2.6 | 3.5
 | 1280 | 650 | 838 | 770 | 714
 | 2770 | 1107 | 1484 | 1380 | 1640
Atomic radius (pm) | 112 | 160 | 197 | 215 | 222
Lonic radius (pm)* | 31 | 651 | 99 | 113 | 135
First ionization energy (kJ/mol) | 899 | 738 | 590 | 548 | 502
Second ionization energy (kJ/mol) | 1757 | 1450 | 1145 | 1058 | 958
Electronegativity | 1.5 | 1.2 | 1.0 | 1.0 | 0.9
Standard reduction potential (V)† | ─ 1.85 | ─ 2.37 | ─ 2.87 | ─ 2.89 | ─ 2.90

## Slide 40: 24.6 The Alkaline Earth Metals (2)
Magnesium
The chemistry of magnesium is intermediate between that of beryllium and the heavier Group 2A elements.
milk of magnesia

## Slide 41: 24.6 The Alkaline Earth Metals (3)
Calcium
a quick lime
slaked lime

## Slide 42: 24.7 Aluminum
Topics
Aluminum

## Slide 43: 24.7 Aluminum (1)
Aluminum
Aluminum is usually prepared from bauxite, which is frequently contaminated with silica , iron oxides, and titanium(IV) oxide.

## Slide 44: 24.7 Aluminum (2)
Aluminum
The Hall Process

## Slide 45: 24.7 Aluminum (3)
Aluminum
The Hall Process
Anode (oxidation): 3
Cathode (reduction): 4
Overall: 2Al2O3

## Slide 46: 24.7 Aluminum (4)
Aluminum
Although aluminum is considered an active metal, it does not react with water as do sodium and calcium.
Reactions:

## Slide 47: 24.7 Aluminum (5)
Aluminum
Thermite Reaction

## Slide 48: 24.7 Aluminum (6)
Aluminum
Aluminum chloride exists as a dimer:
Each of the bridging chlorine atoms forms a normal covalent bond and a coordinate covalent bond (each indicated by an arrow) with two aluminum atoms.

## Slide 49: 24.7 Aluminum (7)
Aluminum
Each aluminum atom is
assumed to be
sp3-hybridized, so the
vacant sp3 hybrid orbital can accept a lone pair from the chlorine atom.

## Slide 50: 24.7 Aluminum (8)
Aluminum
Aluminum chloride undergoes hydrolysis as follows:

## Slide 51: 24.7 Aluminum (9)
Aluminum
Aluminum hydroxide, like Be(OH)2, is amphoteric:

## Slide 52: 24.7 Aluminum (10)
Aluminum
When an aqueous mixture of aluminum sulfate and potassium sulfate is evaporated slowly, crystals of are formed.
Similar crystals can be formed by substituting or or for , and or for .

## Slide 53: 24.7 Aluminum (11)
Aluminum
These compounds are called alums, and they have the general formula
: , ,
: Al Fe3+
Alums are examples of double salts—that is, salts that contain two different cations.

## Slide 54: 24.1 Occurrence of Metals (1) - Appendix
Occurrence of Metals

## Slide 55: 24.2 Metallurgical Processes (10) - Appendix
Steelmaking

## Slide 56: 24.2 Metallurgical Processes (16) - Appendix
Purification of Metals
Electrolysis
Anode (oxidation):
Cathode (reduction):

## Slide 57: 24.2 Metallurgical Processes (17) - Appendix
Purification of Metals
Zone Refining

## Slide 58: 24.3 Band Theory of Conductivity (2) - Appendix
Conductors

## Slide 59: 24.3 Band Theory of Conductivity (4) - Appendix
Semiconductors

## Slide 60: 24.3 Band Theory of Conductivity (5) - Appendix
Semiconductors
n-type semiconductor p-type semiconductor